INVESTIGATION OF W501FD ROW 7 COMPRESSOR BLADE FAILURE AT ENRON GLEASON UNIT 1

October 12, 2000

ABSTRACT

The most probable mode of fracture of a row 7 compressor rotor blade airfoil was high cycle fatigue (HCF).  Cracking initiated at the leading edge (LE) of the airfoil in an area of mechanical damage.  The mechanical damage appeared to be due to impact of FOD during engine operation, prior to the initiation of the fatigue.

1.0 BACKGROUND
A large fragment of an Enron Gleason Unit 1 W501FD Row 7 compressor rotor blade, PN 2072J8/2072J21, position #22 that had fractured through the airfoil was found in the turbine exhaust system.  This report only deals with the loss of a row 7 compressor rotor blade.

2.0 GENERAL INFORMATION
Customer


Enron

Site



Gleason, Tennessee

Unit



1

Frame



W501FD

Unit S.O.#


37A8046

Date of discovery

July 12, 2000

Component name

Rotor blade

Row



7

Component PN

2072J8/2072J21

Position #


22

Total load hours

139

Attempted starts

53

Successful starts

38

Normal shutdowns

35

Fast shutdowns

20

Trips



9

3.0 DESCRIPTION OF FAILURE
The airfoil fracture was located ~75 mm (3.0 inches) above the root platform (Figure 1).  The region of mechanical damage at the airfoil LE measured ~1.3 mm (0.050”) in the span-wise direction and ~1.8 mm (0.070”) in the chord-wise direction (Figure 2).  The damage appeared to be the result of an impact on the airfoil pressure side leading edge, with a 
~0.5 mm (0.020”) deep depression.  The directionality of the impact damage was consistent with engine operation and it appeared to have occurred prior to the initiation of fatigue.  The HCF failure initiated at this FOD location and the fatigue portion of the fracture extended ~65 mm (2.6”) from the leading edge (Figure 3).  As expected, the final fracture of the airfoil was due to overstress.

[image: image1.jpg]f IIIIIIIIHIIIHIIHI'IH

| centiMerens’

, No. 09016 ¢
PRATEO W USA

' ||I|I||Il|ll||||l|l||IIII|I|l'||l||l|l||||l|l|

mcnu

rlllnlrlnlnhhl A





Figure 1: Photograph showing the recovered portions of the Row 7 compressor blade #22 and the fracture height.

[image: image2.jpg]’II|IlIlH,IHl[llH[llllﬂﬂ[lﬂl[lIIIIIIHIHIITHIl||I|||I||I|I||I|||l||l||||IIIl[IIIII|II|]I|I|,II|||II|l||||I|IIII|H|I|IIII|II|IIII |IIII[ll‘|!|Il\
CENTIMETERS :




[image: image3.jpg]



Figure 2: Photographs showing the fatigue fracture length.

[image: image4.jpg]



[image: image5.jpg]



Figure 3: Photographs showing the mechanical damage on the airfoil LE.

4.0 INVESTIGATION

ANALYTICAL MODELING

Analyses were performed in order to determine the source of the HCF failure.  With the mechanical damage at the airfoil LE the analytical model illustrates that the airfoil is susceptible to fatigue fracture at this location.

MANUFACTURING HISTORY

Row 7 compressor blades are manufactured from PD-Spec 10705BR (AISI 616) martensitic stainless steel and receive an aluminum-rich coating per Process Specification 83342NU.  The Enron Gleason Unit 1 row 7 blade that fractured throughout meets the above specification.  There are no rotor blade related non-conformances listed for these parts.

METALLOGRAPHIC EXAMINATION

Scanning electron microscope (SEM) examination of the fatigue surface (Figure 4) confirmed features indicative of HCF.  A potential transverse tear resulting form the impact damage was observed.  Metallographic examination of a planar section through the airfoil LE fracture surface (Figure 5) revealed a transgranular crack path typical of fatigue.

[image: image6.png]



Figure 4: SEM photographs of mechanical damage at airfoil LE.  Arrow indicates direction of fatigue progression.

[image: image7.png]



Figure 5: Optical photomicrographs of planar metallographic section through airfoil fatigue fracture surface and mechanical damage at leading edge.

Fatigue Fracture





Fatigue Fracture





Mechanical Damage








