# CONSERVATION REPORT

ACC #: TR626-2001, TR631-2001, and TR634-2001

##### COLLECTION: Private Collection: Jeff Shankman, 1818 South Blvd, Houston, TX 77098; 713 853.1761wk

CONSERVATOR: C. Shelton

DATE: July 10, 2001

Notes: Objects to be treated for “Defining Modern: European Design 1880-1930”

CONDITION:

TR 626-2001: Charles Ashbee, Two-Handled Coupe with Spoon and Green Glass Liner, c.1900.

The lid and base are moderately tarnished with an unusual copper-colored hue.  There are numerous small scratches and small dings, particularly on the inside, consistent with use.  The glass liner is mildly soiled.  The mother of pearl elements are well seated.

TR631-2001: Paul Follot, Five-Piece Silverplate Tea Service, c.1904.

All of the surfaces are moderately tarnished.  The bottoms of the service items and the tray have noticeable scratching from use. There is a small raised dent in the side of the sugar bowl.  There are several small areas of bubbling in the silver plate on the tops of the lids.  The series of air holes around the bottoms of the handles are filled with a pink polishing compound.

TR634-2001: La Maison Desny, Nickel-Plated Brass Centerpiece, c.1927-28.

All of the plated surfaces are mildly soiled and have handling marks.  There are small scratches and dings consistent with use; the plate is worn off on the bottom of the foot.

TREATMENT PROPOSAL

The treatment proposed for these objects is common practice at the MFAH.  In general, the protocols for cleaning silver, silver plate and nickel or chrome surfaces is identical; however, since the Ashbee coupe has mother of pearl elements, extra care will be taken to keep these elements from coming in contact with solvents or water.

The surfaces will be degreased with mineral spirits and acetone solvents to remove hand oils, wax, and polish/rouge binder residues.  Imbedded polish compounds will be dislodged with a soft bristle brush or soft wood skewer.

The tarnished surfaces will be polished with a slurry of precipitated chalk, de-ionized water and a non-ionic detergent.  This polish material is very soft and has been proven to remove silver tarnish effectively with very little if any disruption of the silver substrate.  This same polish could also be used to remove brass corrosion resulting from loss of the nickel plating on the Desny Centerpiece if degreasing is not adequate.

The surfaces will be washed again with a non-ionic detergent solution, rinsed and dried.  They will be wrapped in tissue and placed in plastic bags until the exhibition.

AUTHORIZATION

Chris Shelton		Date			Jeff Shankman		Date

# TREATMENT REPORT

OBJECT:

COLLECTION/OWNER:

ACC #:

PERIOD:

MAKER:

MATERIALS: appearance of (primary), (secondary)

DESCRIPTION:

CONSERVATOR:		(examining)     (treating)

DATE:

OVERVIEW:

MATERIALS:

HOURS:

DOCUMENTATION:

[ ] 35mm B/W (contact sheet and film in object file)

[ ] 35mm Color Slides (retained by the conservators)

[ ] x-radiographs

[ ] paint/finish/wood or fiber samples